Assisted-Reverse Electrodialysis for permeate remineralization from surface water RO brines: experimental investigation with multi-ionic solutions

Antonia Filingeria,b, Marc Philibertc,*, Emmanuelle Fillouxc, XXX, Alessandro Tamburinia,b, Andrea Cipollinaa,b,*, Giorgio Micalea

a Dipartimento di Ingegneria, Università degli Studi di Palermo, Viale delle Scienze Ed. 6, 90128 Palermo, Italy.

b ResourSEAs SrL, Viale delle Scienze, Ed.16, 90128 Palermo, Italy.

c SUEZ - CIRSEE, 38, rue du Président-Wilson, 78230 Le Pecq, France.

*Corresponding Authors. E-mail: andrea.cipollina@unipa.it, marc.philibert@suez.com

# Abstract

The Assisted-Reverse Electrodialysis (A-RED) process has been proposed as a remineralization strategy for river water RO permeate through direct recovery of minerals from its retentate brine. In the present work, the behaviour of an A-RED unit fed by multi-ion solutions including sodium, chlorides, calcium, magnesium, potassium, sulphates and bicarbonates was assessed. The effect of brine and permeate conductivities and ionic compositions was investigated using a laboratory-scale stack operated/operating at different applied voltages and investigate ion-exchange membrane transport properties through the estimation of apparent ion transport numbers and membrane selectivity.

Results highlighted that the use of calcium or sodium chloride guaranteed higher currents, followed by potassium chloride, while the presence of magnesium chloride, sodium sulphate or sodium bicarbonate resulted in higher stack resistance. Apparent transport numbers were independent of brine and permeate conductivities as well as applied voltage/current, while brine composition mainly affected transport numbers and selectivities. For both two- and three-salt solutions, the selectivity of the cationic exchange membrane decreased as the concentration ratio between the generic ion and sodium increased. In contrast, the anionic exchange membrane selectivity remained constant at ~0.6 and ~1.4 for bicarbonate and sulphate, respectively, although the concentration ratio changed.

These results provided deeper insight into/on ionic exchange membrane ion transport phenomena and in particular ion competition. These data are particularly valuable for the development and widespread application of river RO permeate remineralization using A-RED technology.

Keywords: multi-component solutions, brine valorization, post-treatment, desalinated water, remineralisation, brine disposal, desalination.

# 1. Introduction

Reverse Osmosis (RO) is gaining interest in the field of surface water potabilization [1,2] in addition to its well-established brackish and seawater desalination applications [3,4]. However, desalination processes result in the production of i) mineral-less treated water, the permeate and ii) a concentrated solution, or brine, which is usually discharged.

RO plants for surface water desalination can achieve up to 90% recovery, producing brines that are much more concentrated than the original solution and enriched in microcontaminants or trace elements present in the resource. This concentrated solution is often discharged into sewers or rivers [5], which requires special permits and can contaminate the surrounding environment. Other options are to further concentrate the salts for subsequent recovery using evaporation ponds or disposal through deep-well injection [6]. Conversely, a Zero Liquid Discharge (ZLD) strategy can be a promising option to both treat and valorize the remaining brine, thereby reducing environmental problems [7].

The permeate produced by RO units is very low in total dissolved solids (TDS), tasteless and aggressive [8]. Therefore, the permeate is usually treated to modify its pH, alkalinity and mineral content. Such post-treatment is important for human health [9], to prevent corrosion of pipes [10] and even to improve the taste of drinking water [11,12]. Remineralisation is often achieved by permeate contact with beds of calcium carbonate particles, enhanced by a pre-acidification step (often achieved by CO2 addition) [13], and followed by a pH adjustment step with an alkaline solution [14,15]. Although the process has been known for several years [16], laboratory and pilot scale [17,18] studies are being carried out to develop column contactor design models or particle dissolution models. In addition, other remineralisation methods are being explored, such as the use of white marble in Cameroon [19], the use of dolomite [20], no CO2 addition followed by pH adjustment in Daoura [21] and the use of micronized calcite slurry [22]. However, the most common method is the addition of Ca(OH)2 and CO2 to achieve hardness and alkalinity targets simultaneously [23]. The alternatives to adding reagents such as Ca(OH)2+NaHCO3 or CaCl2+NaHCO3 can be more expensive [14]. Finally, blending with groundwater could be a low cost solution [24], although it could lead to the addition of microbiological content, algae, bacteria, drugs or pesticides that may be present in the feed water [25,26].

Most of these remineralisation techniques rely on the addition of minerals using external chemical reagents, which require procurement and present risks associated with transport to the site and handling, while the minerals necessary for remineralisation are already present in the brine produced in the same plant [27]. Processes making use of this specificity have been developed such as a patented RO permeate remineralization process involving the use of a bivalent ion rich solution extracted from the same feed stream [28]. The innovative use of Assisted-Reverse Electrodialysis (A-RED) to remineralise surface water RO permeates by recovering minerals from the corresponding RO brine was recently presented [29]. This process is based on the use of ion exchange membranes that allow ions to pass selectively from the brine to the permeate while rejecting large molecules such as pesticides or pharmaceuticals that could contaminate the drinking water (see Figure 1). The proof of concept has already been demonstrated using synthetic and real bicarbonate-rich solutions produced by a Low Pressure Reverse Osmosis plant [30]. The economic feasibility of the process at industrial scale was assessed through a parametric techno-economic analysis performed via a simplified model considering the brine as a pure sodium bicarbonate solution [31]. Despite the promising results of previous tests and the simplified techno-economic analysis, a detailed study of process performance and selective transport of the desired ions for permeate remineralisation is still lacking when using multi-ionic mixtures.

Figure 1. Scheme of the Assisted-Reverse Electrodialysis application for river water RO permeate remineralization through the recovery of minerals from RO brine (adapted from [31]).

Electro-membrane processes have recently been investigated in hybrid configuration as pre- or post-treatment steps of desalination (often RO) units to increase plant recovery [32], reduce energy consumption [33,34] or valorise the remaining brine [35]. Electrodialysis (ED) [36] stacks are based on the presence of several repeating units, called cell pairs, terminated by two electrodes, a cathode and an anode. A cell pair consists of a cation exchange membrane (CEM), an anion exchange membrane (AEM) and two spacers that separate the alternating membranes and create the channels for the flow of a diluate and a concentrate solution [37]. When an electric field is applied, cations move towards the cathode, passing through the CEM and being rejected by the subsequent AEM; conversely, anions cross the AEM moving towards the anode, but are blocked by the following CEM. Thanks to the selective action of the ion exchange membranes (IEMs), ions are removed from the diluted compartment and retained in the adjacent concentrated compartment. Electrodialysis is a well-known process whose main application is brackish water desalination, although research is focused on investigating higher performance membranes and optimising operating conditions to make ED a cost-effective process for seawater desalination [38,39]. Reverse Electrodialysis (RED) is a more recent electro-membrane process that is based on the same configuration as the ED stack, but it is operated in the opposite way: it uses the controlled mixing between two solutions being at a different concentration to produce spontaneously energy that can be used to supply an external load [40,41]. In the A-RED process [42] the spontaneous ion flux from the brine to the permeate exploited in RED is enhanced by the application of an external voltage like in ED.

While electro-membrane processes have been widely tested with synthetic solutions of one salt, most commonly NaCl, there has been a great deal of interest in recent years in studying membrane performance in the presence of multiple ions. Several studies focused on the modification/design of new membranes with greater selectivity to ion passage. Regarding the use of AEM, different types of crosslinked AEMs were prepared and compared in terms of chlorides versus sulfates selectivity showing values ranging from ~1 to ~5 depending on the type of AEM [43]. A modified AEM was synthesized to separate selectively chlorides from sulphates from a mixed solution [44]; the authors reached a separation factor (ratio between chlorides and sulphates fluxes) of 5.7, which was much higher compared to the commercial FAB-PK-130 membrane. Golubenko and Yaroslavtsev [45] studied Cl/SO4 selectivity in surfate-sulfonated AEMs obtaining an increasing trend with current and reaching a maximum value of 5.5. Different AEMs were fabricated for selective separation of mono/divalent anions [46]. The chlorides selectivity with respect to sulfates of the DSA AEM was increased up to 47, probably due to both the pore-size sieving effect and electrostatic repulsion. Regarding CEM transport studies, RALEX CEM were modified with sulfated zirconia to increase calcium versus sodium separation efficiency in water treatment [47]. However, the work is mainly focused on the effect of current on transport numbers and ion permselectivity, demonstrating a higher Ca/Na selectivity for doped membranes up to 3.8, obtained at low current density/limiting current density ratio. Zwitterion structured CEM showed higher Na/Mg selectivity due to the presence of carbolic acid, sulfonic acid groups and quaternary ammonium groups that enhanced the transport of sodium to a permeability of up to 58 [48].

Experiments with multi-ion solutions were also performed on entire ED stacks, using both modified and commercial IEMs. Monovalent selective ED process was studied for treating groundwater for irrigation [49] investigating membrane selectivity for calcium and magnesium versus the reference sodium ion. The authors observed an increasing trend of both calcium and magnesium selectivities as function of the applied current density, although in all the tested conditions, divalent selectivity values remained below 1, representing a preferred transport of sodium, followed by calcium and then magnesium. Limiting current density was proposed as a selective promoter for ion removal from multi-ionic mixture, using Commercial Selemion CMVN and ASVN, as cation and anion exchange membranes [50]. The authors observed that chlorides and fluorides were selectively separated with respect to sulphates with a separation efficiency of 0.93 and 0.81, respectively, at the optimal current density. A theoretical electrodialysis model for sodium and potassium mixtures was developed and validated with experiments performed with a laboratory-scale unit, equipped with 10 cell pairs, using solutions containing only sodium nitrate and a mixture of sodium and potassium nitrates [51]. The authors observed that electromigration transport resulted in the main contribution to ion transport while the diffusion mechanism could switch the selective transport of ions due to the opposite contribution to the two ions.

Ion transport through IEMs was explored for brackish water desalination [52,53] and wastewater treatment [54] of greenhouses to selectively concentrate the solution in the divalent ions  calcium, magnesium and sulfates by preferentially removing monovalent ions of sodium, chlorides and/or nitrates. Monovalent-selective electrodialysis (MSED) technology was tested with Neosepta and Fujifilm Type 16 membranes focusing on ion transport and membrane selectivity. Results demonstrated overall moderate larger selectivity towards sodium for the Neosepta membranes [54] with a decreasing trend of cation selectivity when the cation ratio increased for brackish water desalination [52] or no linear relationship between ion selectivity and ions concentration [54].

Xu et al. [55] compared monovalent permselective CEM (CR671) with normal grade CEM (CR67) for brackish groundwater desalination at both bench and pilot scale. The authors observed a sodium selective transport respect to divalent cations, as well as calcium and magnesium, up to 9 times higher for the pilot unit at low current density while the performance difference between Na-selective CR671 and normal-grade CR67 diminished at high current density. However, they only analyzed CEM permselectivity of calcium and magnesium compared to sodium with a fixed solution composition. With the same type of IEMs, Xu et al. [56] investigated the use of an ED pilot unit to treat brackish water RO concentrate solutions. They observed a relative transport number of potassium, calcium and magnesium compared to sodium approximately equal to 1.7, 2 and 3 respectively, in the investigated current density range. A pilot scale EDR system was tested for treating water for golf-course irrigation [57] demonstrating that the equivalent removal of divalent ions as calcium and magnesium compared to the monovalent sodium was dependent on current density and water recovery with the relative transport number of calcium versus sodium ranging between 5.5 and 1.7 and sulfates versus chlorides between 1.5 and 2.6, depending on the operating condition.

Although electro-membrane processes have been extensively characterized with single salt solutions and some progress has been made in the case of multi-ionic mixtures, tests have often focused on characterizing a single membrane or a limited number of ions and operating conditions. In fact, an effective description of ion transport obtained from simple experiments with real units containing both CEM and AEM, providing a complete and detailed description of ion transport and membrane selectivities, is still rare. This work aims to fill this gap, in particular for the use of A-RED units, which have been poorly tested with multi-ion solutions, for the novel application of river water RO permeate remineralization by transporting ions from its brine. With this respect, an experimental campaign was carried out using a laboratory-scale A-RED stack fed with synthetic solutions containing two or three competing ions. The effect of applied voltage as well as brine and permeate conductivities and a wide range of compositions were tested. In addition, membrane transport numbers and selectivity were assessed, highlighting potential applications of the technology for mineral recovery.

# 2. Materials and methods

A-RED tests were conducted in open-loop mode with synthetic multi-ionic solutions, containing two or three salts at different composition. This section presents the materials and system set-up (section 2.1), the experimental procedure (section 2.2), experimental campaign (section 2.3) and data analysis (section 2.4).

### 2.1 Materials and set-up

Experiments were performed with an A-RED laboratory-scale unit (ElectromatTM MkI SUEZ France stack), assembled with five cell pairs of CR67T and AR204T SUEZ membranes having 0.028 m2 of active membrane area. Spacers of 760 µm thickness (woven polyester) were placed between membranes. Coated titanium electrodes with a flat surface were used. Table 1 reports membrane characteristics and properties. Platinum wires (Alfa Aesar Pt wires, 0.127 mm dia hard, 99.9% metal basis) were included during the stack assembly.

Table 1. Properties of the SUEZ ion-exchange membranes used in this study (SUEZ, France).

|  | Thickness (dry) [µm] | Areal resistance [Ω cm2] | Permselectivitya [%] | IECb [meq/g] | Stability pH |
| --- | --- | --- | --- | --- | --- |
| AEM: AR204T CEM: CR67T | 280 300 | 1.7 2.5 | 89 86 | 2.43b 2.55b | 1 - 10.5 1 - 14 |

a Obtained from OCV measurements at 0.5/1.0 M NaCl.

b Expressed as meq/dry g resin.

The experimental campaign was composed of three different phases: i) tests with single-salt solution (i.e., NaCl, NaHCO3 and CaCl2) that were reported and discussed in our previous paper [30], ii) tests with two salts solutions, and iii) tests with three mixed salts solutions. For mixed-salts trial runs, the combinations were carefully selected to obtain two/three competing cations with a unique joint anion (i.e., NaCl – CaCl2, NaCl–MgCl2 and NaCl – KCl for two salts tests and NaCl – CaCl2 – MgCl2 for three salts tests) or two/three competing anions and a fixed cation (i.e., NaCl – NaHCO3 and NaCl-Na2SO4 for two salts solutions and NaCl – Na2SO4 – NaHCO3 for three salts solutions). Sodium and chlorides were thus considered as the reference ion among cations and anions, respectively. Synthetic solutions were prepared in 250L tanks with demineralized water and single salts as NaCl (Laboratory grade, VWR Chemicals BDH®), CaCl2 (93% purity, Alfa Aesar), MgCl2 (>95% purity, Aldrich® Chemistry), KCl (>99% purity, Sigma-Aldrich®), NaHCO3 (>99.7% purity, VWR Chemicals BDH®), Na2SO4 (AnalaR NORMAPUR® Reag., VWR Chemicals). The electrode rinse solution (ERS) was composed of a 0.25 mol/L Na2SO4 solution, recirculated in closed-loop through both cathode and anode compartments. Figure 2 shows a schematic representation of the experimental setup. Gear Drive pumps (Micropump GA-T23.PFS.A) were used to feed both brine and permeate solutions in continuous mode and ERS in closed loop. Inlet pressure was monitored using pressure gauges (Cewal), placed before the stack entrance. Online rotameters were installed after the stack to continuously monitor solution flowrates, which were periodically checked during each test with offline manual measurements. Electrodes were connected to a DC power supply (1902B, B&K precision) and two multimeters (Fluke 115) were connected in series and parallel to the stack to measure the electric current and the voltage, respectively. The conductivities of the inlet and outlet solutions were measured using a portable conductivity meter (WTW 314i), while samples of both solutions were taken for further ionic composition analysis using different instrumentation depending on the type of ion (850 professional IC, Metrohm; ICP-OES 5110, Agilent; Titrando 809 Metrohm).

Figure 2. Schematics of the A-RED set-up with some auxiliaries and picture of the stack (adapted from [30]).

### 2.2 Experimental procedures and analytical techniques

Internal and external leakage tests [58] were performed after assembling the stack to ensure a negligible effect of leakage on the unit’s performance. Each time the solution was changed (i.e., different composition and/or conductivity), membranes in the stack were equilibrated with the feed solution at least overnight without applying any voltage to ensure stability to the process.

Experiments were performed in open-loop mode for both solutions in parallel flow at a velocity of ⁓2 cm/s (flow rates of 18 L/h) while the ERS was maintained in closed-loop mode. Before starting the test, inlet solution conductivities as well as Open Circuit Voltage (OCV) were measured. Then, increasing steps of voltage were applied to the stack for at least 8-10 times the residence time of the solution in the stack to ensure steady-state conditions. For each step of voltage, the corresponding current was recorded as well as the exiting solution conductivities, temperatures and flowrates. Voltage measurement was performed both at the electrodes and at the platinum wires. The first measurement represents the overall voltage applied to the stack (including both the voltage drop at the electrode compartments and the fraction of voltage effectively applied to the 5 cell pairs). The voltage measured at the platinum wires strictly represents the 5-cell pairs voltage and is extremely important because it excludes the voltage of the electrodic compartments, which has a significant effect on the laboratory stack with only 5 cell pairs, whereas it would be almost negligible on a pilot/industrial scale. From these data points, current density-voltage and conductivity-current density curves were built to estimate the effect of different ions on desalination performance and stack resistance (i.e., the slope of the current density-voltage curve). Furthermore, for tests with single salt solutions, the salt concentrations were calculated from the conductivities through the use of empirical correlations. For tests with multi-ionic solutions a more complete composition analysis was conducted for both anions and cations to study the specific ion transport at different applied voltages and brine compositions.

Several tests were repeated during the experimental campaign to study results reproducibility. All tests were carried out at room laboratory temperature (T=17-20°C). Mass and charge balances were verified to be within an error of less than 15%, that was estimated to be the experimental error due to the ion analysis instruments used in this work.

### 2.3 Experimental campaign

Tests were carried out at inlet conductivity of 1200 µS/cm and 3000 µS/cm for the brine solution and 70 µS/cm, 300 µS/cm, and 1000 µS/cm for the permeate stream. The brine conductivities were chosen to match the brine exiting from a real three stage RO treated Seine river water which was mainly constituted by: Ca2+ (600 mg/L), Na+ (65 mg/L), Mg2+ (51 mg/L), K+ (22 mg/L), HCO3- (1400 mg/L), SO42- (330 mg/L), Cl- (170 mg/L), and NO3- (140 mg/L), at a conductivity of ~3030 µS/cm. Brine conductivity of 1200 µS/cm was also tested to mimic the conductivity of the brine entering the stack in a feed & bleed configuration in which part of the outlet more diluted brine is recirculated and mixed with RO-brine. The permeate conductivity range was selected to mimic the real operating condition of an A-RED unit for permeate remineralization in which a recirculation configuration will probably be adopted to reduce specific energy consumptions and costs [31]. Part of the experimental campaign was performed by varying inlet permeate conductivity at i) 70 µS/cm, ii) 300 µS/cm, and iii) 1000 µS/cm to investigate its effect on ion transport through IEMs. On the basis of the results obtained, the second part of the experimental campaign was performed with an inlet permeate conductivity of 70 µS/cm.

Furthermore, for each inlet conductivity couple, tests with two/three competing ions were carried out starting with a reference composition obtained by assuming that the ratio between the generic cations/anions and the reference sodium/chlorides was the same as the Seine river RO brine. Furthermore, for the inlet conductivity couple brine-permeate of 3000-70 µS/cm, two other compositions were tested to study the effect of the inlet composition on the performance of the A-RED unit. Table 2 and

Table 3 summarize all the operating conditions tested in the present work for competition among the cations and anions, respectively. The corresponding ion concentration was adjusted to match the desired conductivity.

Table 2. Operating conditions: inlet conductivities and ion ratio for both brine and permeate feed solutions for tests with competing cations.

| Salt | Inlet brine conductivity [mS cm-1] | Inlet permeate conductivity [mS cm-1] | Generic cation respect to Na+ [mol/mol] |
| --- | --- | --- | --- |
| NaCl - CaCl2 | 3.0 | 0.07 | ≈ 5.3 ≈ 1.0 ≈ 0.2 |
|  | 3.0 | 0.3 1.0 | ≈ 5.3 |
|  | 1.2 | 1.0 |  |
| NaCl - KCl | 3.0 | 0.07 | ≈ 5.0 ≈ 1.0 ≈ 0.2 |
|  | 3.0 | 0.3 | ≈ 0.2 |
|  | 1.2 | 1.0 |  |
|  | 1.2 | 1.0 |  |
| NaCl - MgCl2 | 3.0 | 0.07 | ≈ 5 ≈ 0.2 ≈ 0.2 |
|  | 3.0 | 0.3 | ≈ 0.7 |
| NaCl - CaCl2 - MgCl2 | 3.0 | 0.07 | - Mg/Na ≈ 0.7 and Ca/Na ≈ 4.4 - Mg/Na ≈ 0.2 and Ca/Na ≈ 1 - Mg/Na ≈ 0.2 and Ca/Na ≈ 0.2 |
|  |  | 0.3 | Mg/Na ≈ 0.7 and Ca/Na ≈ 4.4 |

Table 3. Operating conditions: inlet conductivities and ion ratio for both brine and permeate for tests with competing anions.

| Salt | Inlet brine conductivity [mS cm-1] | Inlet permeate conductivity [mS cm-1] | Generic anion respect to Cl- [mol/mol] |
| --- | --- | --- | --- |
| NaCl - NaHCO3 | 3.0 | 0.07 | ≈ 4.7 ≈ 1.0 ≈ 0.2 |
|  | 3.0 | 0.3 | ≈ 4.7 |
|  | 1.2 | 1.0 |  |
| NaCl - Na2SO4 | 3.0 | 0.07 | ≈ 5 ≈ 1.4 ≈ 0.4 |
|  | 3.0 | 0.3 | ≈ 1.4 |
| NaCl - NaHCO3 - Na2SO4 | 3.0 | 0.07 | - HCO3/Cl ≈ 4.7 and SO4/Cl ≈ 0.7 - HCO3/Cl ≈ 0.2 and SO4/Cl ≈ 0.2 - HCO3/Cl ≈ 1 and SO4/Cl ≈ 0.7 |
|  |  | 0.3 | HCO3/Cl ≈ 4.7 and SO4/Cl ≈ 0.7 |

### 2.4 Data analysis

The experimental campaign focused on the use of multi-ionic solutions to investigate the membrane behaviour in the presence of more ions. Particularly, the flux of the generic ion, Jion (mol/m2/s), was calculated from the mass balance as reported in the following equation:

| Jion=QPerm(CPerm,ion,OUT-CPerm,ion,IN)Amemb | (1) |
| --- | --- |

where QPerm (L/s) is the permeate flowrate, CPerm,ion,IN (mol/L) and CPerm,ion,OUT (mol/L) are the concentration of the generic ion at the inlet and outlet section of the stack, and Amemb (m2) is the membrane area. This flux represents the net apparent flux, including migrative and diffusive phenomena. However, it is important to note that diffusive effects are negligible compared to migrative ones due to the small concentration gradient between the concentrated and dilute solutions. In addition, this gradient decreases along the length of the stack as ions move from the concentrated to the dilute compartment in the A-RED process.

The apparent transport number, tion (-), of the generic ion was calculated as the ratio between the generic ion flux and the total flux, as:

| tion=JionzionionJionzion | (2) |
| --- | --- |

where zion is the ion valence. Specifically, the ion transport number was calculated separately for cations and anions that move through the CEM and AEM, respectively.

An important parameter to quantify the selectivity of each membrane to the specific ion is the membrane selectivity, Selrefion (-), here defined as the ratio between the transport numbers of the generic and reference (ref)) ionsref normalized by the ratio between the inlet equivalent concentration of the same ions in the brine compartment [54]. In formula:

| Selrefion=tiontrefzionzrefCBrine,ionCBrine,ref | (3) |
| --- | --- |

where CBrine,ion and CBrine,ref are the concentrations of the generic and reference ions in the brine compartment. More in detail, sodium was selected as the reference ion among the cations for the analysis of transport phenomena and selectivity of the CEM. Similarly, chloride was chosen as reference ion among the anions for examining AEM selectivity. Selectivity for the reference ion will always be equal to 1 while a selectivity of a generic ion equal to 1 will represent a membrane that allows the ion to pass with the same affinity as the corresponding reference ion. Selectivities above 1 will represent a CEM/AEM with a better affinity to other ions than Na/Cl.

# 3. Results and discussion

Results are here divided into two different sub-sections. Sub-section 3.1 focuses on the comparison among tests performed with two salts solutions, containing two competing ions. Sub-section 3.2 discusses the performance when three different salts are used.

### 3.1 Results for tests with two mixed salts

Figure 3a reports platinum wires voltage-current density curves for experiments performed with i) single-salt solutions, and ii) two-salt solutions at inlet conductivity of 0.07 mS/cm and 3.0 mS/cm for permeate and brine, respectively. All tests, with one or two salts, were prepared at the same conductivity for both permeate and concentrate channels. For the sake of simplicity, the ion concentration ratios reported in the graph are the same as that of the real Seine river RO brine; indeed the effect of the different ion concentration ratio on the platinum wire voltage-current density curves was negligible. Results for single-salt solutions were already reported in our previous work [30] but are presented here with the use of platinum wire voltage that facilitates the comparison among experiments with single- and two-salt solutions. For all experiments, the current density increased with the applied voltage as expected. Among the single-salt solutions, the use of NaCl or CaCl2 resulted in similar performances reaching the highest current density obtained at the operating condition of this work. In other words, the CEM affinity to the passage of Na+ or Ca2+ remained similar, hence the same resulting current was observed. Conversely, for single-salt tests in which a different anion is considered (NaCl or NaHCO3 only), a clear difference was observed for all applied voltages. Indeed, when only HCO3- anions are present in the solution, a lower current density was achieved compared to tests with NaCl that can be attributed to the higher electrical resistance of membranes towards HCO3- than Cl-. At the maximum applied voltage (10 V to the total stack and ~7.7 V to platinum wires), current densities were in the range of 25-37 A/m2. Specifically, 22% lower current was reached with the NaHCO3 single-salt solution. This behavior was confirmed by tests with two-salt solutions. In particular, the use of both NaCl and CaCl2 resulted in a very similar total current to the corresponding single-salt solutions. Similarly, a mixture of NaCl and NaHCO3 resulted in a voltage-current density curve that was between the trend of the corresponding single salt tests. Two salt solutions were tested with NaCl and another with Na2SO4, MgCl2 and KCl as these ions were present in the real brine produced by the RO unit treating Seine river water, although in minor concentrations. The mixture of KCl and NaCl salts achieved slightly lower current densities (~9 %) compared to NaCl alone, while the presence of SO42- or Mg2+ ions in the mixture negatively affected the membrane resistance causing a lower total current for any applied voltage. Figure 3b shows the outlet permeate conductivity as a function of the platinum wire voltage. Obviously, the outlet permeate conductivity increased with the applied voltage due to the corresponding increase in the current density, thus ion transport from the brine to the permeate. At the maximum applied voltage, the outlet permeate conductivity was in the range of 0.8-1.2 mS/cm, ensuring  full remineralization. The final conductivity is higher than that required for drinking water since it can be diluted by mixing the outlet permeate solution with a bypass of the RO permeate stream in order to increase the production of remineralized water and reduce capital costs [31]. The conductivity trend showed a qualitatively good agreement with the trend of current density as a function of applied voltage. In fact, the presence of sulphates, bicarbonates and magnesium reduced the current density, thus the outlet permeate conductivity while the presence of sodium, calcium, chlorides and potassium, as single- or mixed-salt solutions, achieved higher remineralization. However, it is important to note that current density is directly correlated to the in-out concentration variation and not with the conductivity. For this reason, the slight difference in the conductivity and current trends, as seen also for potassium, can be attributed to the different conductivity-concentration laws.

Figure 3. a) Platinum wires voltage-current density curves and b) outlet permeate conductivity-platinum wires voltage curves for i) single salt solution (empty symbol, already reported in [30]) and ii) two salt solution (filled symbols). All the tests were performed at inlet conductivity of 0.07 mS/cm and 3.0 mS/cm for permeate and brine, respectively. The composition of the two-salts solution is indicated in the graph.

Figure 4 shows the trend of the transport numbers for two tests with two-salts solutions as a function of current density, brine conductivity and composition. Figure 4a shows the Ca2+ transport number obtained from tests with CaCl2-NaCl in which calcium and sodium cations were in competition while the anion was common to both salts; Figure 4b shows the transport number of HCO3- for different tests performed with the NaHCO3-NaCl mixture where the anions were in competition while the cation was common. Calcium versus sodium and bicarbonates versus chlorides competitions are discussed in more detail in the paper due to their main role in the remineralization objectives. While, transport numbers for the other two-salt solution mixtures (KCl-NaCl, MgCl2-NaCl, and Na2SO4-NaCl) are reported in the Supporting Information section (see Figures S1-S3) and similar conclusions were obtained.

Obviously, the transport number of the competing cation/anion in Figure 4a/Figure 4b, respectively, can easily be obtained as the complement to 1 of the transport number reported in the Figures. Transport number was independent of current density in all the experiments performed. Furthermore, transport numbers were not dependent on brine conductivity when the composition was kept fixed, as it can be observed from tests at inlet brine conductivities of 3000 µS/cm and 1200 µS/cm. Moreover, permeate conductivity had no effect on the transport numbers as can be observed from their constant values for permeate conductivities of 70 µS/cm, 300 µS/cm and 1200 µS/cm. This result can be expected as the ions are transported from the brine to the permeate in the A-RED configuration, so the parameters affecting transport are mainly related to the brine compartment. Indeed, the main effect was obtained when varying the composition of the brine solution. Specifically, as the Ca/Na and HCO3/Cl ratios increased, the transport number of the competitive ion increased too. This behavior can be expected because apparent ion transport numbers are heavily dependent on the ion concentration in solutions. In fact, ions at high concentration in solution are associated with high transport numbers [52,59]. It is interesting to note that for the CaCl2-NaCl solution at equimolar concentration, transport numbers of Ca2+ was ~0.66, demonstrating that CEM has good affinity with this bivalent cation. Indeed, comparing the two tests at Ca/Na ratios of 0.2 and 5 it can be noted that calcium crossed CEM more easily when it was at lower concentrations, in fact, calcium transport numbers were ~0.32 and ~0.81, at ion concentration ratio of 0.2 and 5, respectively. When bicarbonates and chlorides were in competition in a equimolar solution (tests NaHCO3-NaCl test in Figure 4b), bicarbonates transport number was ~0.37 on average, confirming the lower affinity of AEM for bicarbonate, as observed also by the higher stack resistance (lower current) of tests performed with NaHCO3 only with respect to the single NaCl solutions.

Regarding the other two-salt solutions tests (SI Figures S1-S3), it is interesting to note that for KCl- NaCl solution at equimolar concentration, transport number of K+ and Na+ were at ~0.5, demonstrating that CEM has similar affinity to both monovalent cations, As observed for calcium, at approximately equimolar solutions (ion concentration ratio of 0.7), magnesium transport numbers had values above 0.5. Conversely, sulphates ions resulted in a transport number of 0.37 and 0.65 for ion concentration ratio of 0.2 and 0.7.

Figure 4. a) Calcium and b) bicarbonates transport numbers as function of current density for different inlet brine and permeate conductivities and compositions for tests performed with two salts solution: a) CaCl2-NaCl and b) NaHCO3-NaCl .

In order to take into account the effect of the ion concentration in the brine solution, apparent ion selectivities were defined with respect to a reference ion; specifically in relation to sodium for CEM and to chloride for AEM.

Figure 5 reports selectivities of different cations (Figure 5a) and anions (Figure 5b) in competition with the corresponding reference ion, i.e., sodium and chlorides, respectively, as a function of different ion concentration ratios.

Cation selectivities decreased as the concentration ratio increased for all the ions tested in the present work. A similar result was also obtained for multi-ionic brines at different molar ratio tested in electrodialysis with bipolar membrane units to produce acidic and alkaline solutions [59], although with extremely different solution composition and conductivity. Both calcium and magnesium showed higher selectivity compared to sodium likely due to the larger electrostatic attraction between divalent cations and the negatively charged membrane groups [55]. The higher potassium selectivity can be ascribed to potassium’s higher mobility, derived from its larger ionic radius and lower shell of hydration [60]. All cation selectivities were greater than or equal to 1.0 for concentrations below the ion ratio of 1.0. Conversely, when the ion concentration ratio in the brine is very high, i.e. 5.0,  the selectivity reduced in all cases to values less than one (0.8-0.95 depending on the ion). Consequently, these results showed that at least with the membrane tested in this work, in order to enhance the passage of a cation from the brine to the permeate, a compromise must be found between increasing the concentration of the ion in solution and having a high membrane selectivity.

For AEM, a different behavior was observed. In fact, the ion selectivities of both bicarbonates and sulphates remained constant as the ion concentration ratio increased. More specifically, the selectivity of bicarbonate ions was constant at values around 0.6, .This was not the case for the sulphate ion, which maintained a selectivity of about 1.4. Thus, sulphates ions are transported with a higher selectivity compared to chlorides, as observed in [57], despite the higher stack resistance for the complete applied voltage range tested in this work.

The negligible effect of both brine and permeate conductivities on ion selectivities, as expected from the transport numbers trends, is showed in Figure S4 of the Supplementary Information for K+ and HCO3- ions in competition with Na+ and Cl-.

It is important to note that the main goal of remineralization is to add calcium and bicarbonate ions to the permeate coming from the RO unit. In the case of the membranes tested and with reference to the RO brine solution from the Seine river, the passage of the cations of interest remained favored by a selectivity almost equal to or greater than 1, while the transport of bicarbonates was favored by the high concentration of these ions with respect to chlorides. The transport of potassium, sodium, and magnesium is expected to be low due to the very low concentration compared to calcium.

Figure 5. Selectivities as function of the ion concentration ratios for competitive a) cations and b) anions for two-salts solutions. Sodium and chlorides were selected as reference ions among cations and anions, respectively. Inlet brine and permeate conductivities equal to 3.0 mS/cm and 0.07 mS/cm, respectively. Platinum wires voltage ~7.8 V.

### 3.2 Results for tests with three mixed salts

Figure 6 reports platinum wire voltage-current density curves for experiments performed with i) single salt solutions (CaCl2, NaCl, and NaHCO3), ii) two-salt solutions (MgCl2-NaCl, CaCl2-NaCl for graph a, and Na2SO4-NaCl, NaHCO3-NaCl for graph b), and three-salt solution (MgCl2-CaCl2-NaCl in graph a and Na2SO4-NaHCO3-NaCl in graph b). All tests were performed at inlet conductivity of 0.07 mS/cm and 3.0 mS/cm for permeate and brine, respectively, while the ion ratios were varied. For the three cations in competition (see Figure 6a), the presence of magnesium in the mixture, even if at low ion concentration ratio, significantly affected the voltage-current density curve, reaching lower values of current at the same voltage.

Similarly, for the three anions in competition, the presence of sulphates ions in the three-salts solution caused an increase in the total resistance and thus current densities close to the values obtained with the Na2SO4-NaCl two-salt mixture or NaHCO3 alone. The conductivity trend as a function of the applied voltage is reported in the Supplementary information and confirmed the trend obtained with two-salt solutions.

Figure 6. Platinum wires voltage-current density curves for tests performed with three salts solutions with a competition between a) cations (MgCl2-CaCl2-NaCl) and b) anions (Na2SO4-NaHCO3-NaCl). All the tests were performed at inlet conductivity of 0.07 mS/cm and 3.0 mS/cm for permeate and brine, respectively. The composition of the two and three salts solution is indicated in the graph.

Figure 7 shows selectivities trends for cations (graph a) and anions (graph b) in competition with sodium and chlorides, respectively, as a function of ion concentration ratio. Trends for three-salt solutions were compared with the corresponding two-salt mixtures. The precise composition of multi-ion mixtures is reported in Table 3 and ion concentration ratio of 0.7, used for both magnesium and sulphates, is reported as 1 for the sake of comparison. Tests with three-salt solutions confirmed the decreasing trend of cations selectivities as the concentration ratio increased. Indeed, it is interesting to note that the selectivity of calcium with respect to sodium in mixtures of three cations including magnesium was in all cases slightly higher than in the case of two salts solutions. Indeed, the presence of magnesium, which showed a higher selectivity towards sodium than calcium, in the three-salts mixture resulted in a mildly beneficiary effect on calcium selectivity. On the other side, the selectivity of magnesium with respect to sodium in the presence of calcium ions was slightly lower than in the mixture of magnesium and sodium chlorides alone. Therefore, the presence of a third cation in the mixture seemed to slightly affect the ion selectivity compared to the simple two-salts solution case.

Conversely, for mixtures of three competing anions, as observed for two-salts solutions, constant selectivity trends were observed as a function of the ion concentration ratio. In particular, for three-salts solutions, ion selectivities were slightly lower compared to the corresponding selectivity for two salts at the same ion ratio, although such difference is comparable to the experimental uncertainty.

Figure 7. Selectivities as function of the ion concentration ratios for competitive a) cations and b) anions for two and three-salts solutions. Sodium and chlorides were selected as reference ions among cations and anions, respectively. Inlet brine and permeate conductivities equal to 3.0 mS/cm and 0.07 mS/cm, respectively. Platinum wires voltage ~7.8 V.

# Conclusions

The behaviour in Assisted-Reverse Electrodialysis (A-RED) unit with multi-ionic solution for recovering minerals from river RO brine and directly remineralize its permeate was investigated. A laboratory-scale stack and cation and anion exchange membrane (CEM and AEM) transport when two/three-salt solutions were used. The experiments were performed using two or three cations/anions in competition and fixing the same anion/cation, including sodium, chloride, calcium, magnesium, potassium, bicarbonates and sulphates. A reference composition was selected on the basis of a real Seine river RO unit, while the effect of applied voltage/current, brine and permeate conductivities and compositions was studied to investigate the membrane behaviour at different operating conditions. Apparent transport numbers and membrane selectivities were calculated using sodium and chloride as reference ion among the cations and anions, respectively.

The A-RED unit showed similar behaviour when sodium and/or calcium chlorides were used, achieving the highest current density, thus permeate remineralization demonstrating similar CEM affinity to both ions. The use of potassium achieved slightly lower performances, while the presence of magnesium ions resulted in a higher stack resistance. Regarding anions, the presence of bicarbonates and/or sulphates compared to chlorides-only provided 20-25% lower current, demonstrating the higher stack resistance to their transport.

Current density as well as brine and permeate conductivities had negligible effect on membrane properties at the tested operating conditions. Conversely, brine composition had the main effect leading to large variation in transport numbers, i.e. for calcium transport number from ~0.32 to ~0.81 when the calcium versus sodium concentration ratio was increased from 0.20 to 5. Interestingly, cation selectivities were reduced from ~1.9 to ~0.8, on average depending on the ion, as the ion concentration ratio increased. Conversely, AEM selectivities remained constant as the ion concentration ratio increased at values of  ~0.6 and ~1.4 for bicarbonates and sulphates.

This study provided interesting insights into the characterization of ions transport through IEMs in the A-RED unit when multi-ionic solutions are used for mineral recovery from river RO brine and remineralization of its permeate, and may be a first step towards the widespread of its application.

# List of abbreviations

Acronyms

AEM		anion exchange membrane

A-RED	assisted-reverse electrodialysis

CEM		cation exchange membrane

ED		electrodialysis

ERS		electrode rinse solution

IEM		ion exchange membrane

MSED		monovalent-selective electrodialysis

OCV		open circuit voltage

RED		reverse electrodialysis

RO		reverse osmosis

TDS		total dissolved solids

ZLD		zero liquid discharge

Symbols

Amemb (m2) 		membrane area

C (mol/L)		ion concentration

i (A/m2)		current density

IEC (meq/g)		ion exchange capacity

J (mol/m2/s)		ion flux

Q (L/s)			solution flow rate

Selrefion (-)		membrane selectivity

t (-)			transport number

VPt (V)			platinum wires voltage

Greek symbols

σ (mS/cm)		solution conductivity

Subscripts and superscripts

Brine		brine stream

ion		generic ion

IN		inlet

OUT		outlet

Perm		permeate stream

ref		reference ion

# References

[1]	R. López-Roldán, S. Platikanov, J. Martín-Alonso, R. Tauler, S. González, J.L. Cortina, Integration of Ultraviolet-Visible spectral and physicochemical data in chemometrics analysis for improved discrimination of water sources and blends for application to the complex drinking water distribution network of Barcelona, J. Clean. Prod. 112 (2016) 4789–4798. https://doi.org/10.1016/j.jclepro.2015.06.074.

[2]	J. Raich-Montiu, J. Barios, V. Garcia, M.E. Medina, F. Valero, R. Devesa, J.L. Cortina, Integrating membrane technologies and blending options in water production and distribution systems to improve organoleptic properties. The case of the Barcelona Metropolitan Area, J. Clean. Prod. 69 (2014) 250–259. https://doi.org/10.1016/j.jclepro.2014.01.032.

[3]	L.N. Nthunya, M.F. Bopape, O.T. Mahlangu, B.B. Mamba, B. Van der Bruggen, C.A. Quist-Jensen, H. Richards, Fouling, performance and cost analysis of membrane-based water desalination technologies: A critical review, J. Environ. Manage. 301 (2022) 113922. https://doi.org/10.1016/j.jenvman.2021.113922.

[4]	K.H. Chu, J. Lim, S.J. Kim, T.U. Jeong, M.H. Hwang, Determination of optimal design factors and operating conditions in a large-scale seawater reverse osmosis desalination plant, J. Clean. Prod. 244 (2020) 118918. https://doi.org/10.1016/j.jclepro.2019.118918.

[5]	A. Panagopoulos, K.J. Haralambous, M. Loizidou, Desalination brine disposal methods and treatment technologies - A review, Sci. Total Environ. 693 (2019) 133545. https://doi.org/10.1016/j.scitotenv.2019.07.351.

[6]	M. Mickley, Desalination and Water Purification Research and Development Program Report No. 207, Reclaimation Manag. Water West. (2018) 56. https://www.usbr.gov/research/dwpr/reportpdfs/report207.pdf.

[7]	A. Panagopoulos, Techno-economic assessment and feasibility study of a zero liquid discharge (ZLD) desalination hybrid system in the Eastern Mediterranean, Chem. Eng. Process. - Process Intensif. 178 (2022) 109029. https://doi.org/10.1016/j.cep.2022.109029.

[8]	EU Drinking Water Directive, (Council Directive 98/83/EC of 3 November 1998 on the quality of water intended for human consumption), n.d. https://ec.europa.eu/environment/water/water-drink/legislation_en.html%0A%0A.

[9]	L. Bhajan, S. Nallakukkala, Gas Hydrate in Water Treatment, 2022. https://doi.org/10.1002/9781119866145.

[10]	P. Nativ, O. Leifman, O. Lahav, R. Epsztein, Desalinated brackish water with improved mineral composition using monovalent-selective nanofiltration followed by reverse osmosis, Desalination. 520 (2021) 115364. https://doi.org/10.1016/j.desal.2021.115364.

[11]	Y. Shuai, K. Zhang, H. Zhu, J. Lou, T. Zhang, Toward the Upgrading Quality of Drinking Water from Flavor Evaluation: Taste, Feeling, and Retronasal Odor Issues, ACS ES T Eng. (2022). https://doi.org/10.1021/acsestengg.2c00354.

[12]	M.H. Vingerhoeds, M.A. Nijenhuis-de Vries, N. Ruepert, H. van der Laan, W.L.P. Bredie, S. Kremer, Sensory quality of drinking water produced by reverse osmosis membrane filtration followed by remineralisation, Water Res. 94 (2016) 42–51. https://doi.org/10.1016/j.watres.2016.02.043.

[13]	H. Shemer, R. Semiat, D. Hasson, Re-mineralization of desalinated water using a mixture of CO2 and H2SO4, Desalination. 467 (2019) 170–174. https://doi.org/10.1016/j.desal.2019.06.017.

[14]	L. Birnhack, O. Lahav, Post-Treatment of Desalinated Water-Chemistry, Design, Engineering, and Implementation, Elsevier Inc., 2018. https://doi.org/10.1016/B978-0-12-809240-8.00008-3.

[15]	H. Shemer, D. Hasson, R. Semiat, M. Priel, N. Nadav, A. Shulman, E. Gelman, Remineralization of desalinated water by limestone dissolution with carbon dioxide, Desalin. Water Treat. 51 (2013) 877–881. https://doi.org/10.1080/19443994.2012.694236.

[16]	V. Yamauchi, K. Tanaka, K. Hattori, M. Kondo, N. Ukawa, Remineralization of desalinated water by limestone dissolution filter, Desalination. 66 (1987) 365–383. https://doi.org/10.1016/0011-9164(87)90218-9.

[17]	D. Vries, M. Korevaar, S. Ghanbari, G. van Houwelingen, W. van der Meer, Data fusion to monitor remineralisation of desalinated groundwater in calcite contactors, J. Water Process Eng. 41 (2021) 102011. https://doi.org/10.1016/j.jwpe.2021.102011.

[18]	S. Lim, Y.C. Kim, Optimization of pilot-scale re-mineralization by calcite dissolution using sulfuric acid for seawater desalination processes, Environ. Sci. Water Res. Technol. 9 (2022) 620–629. https://doi.org/10.1039/d2ew00768a.

[19]	T.N. Nguemtue, R. Kamga, J.M. Sieliechi, J. Kayem, Evaluation of two white marbles for the correction of the aggressivity of fresh water of rivers, Sci. African. 10 (2020). https://doi.org/10.1016/j.sciaf.2020.e00601.

[20]	J. Dudáš, J. Derco, T. Kurák, N. Šoltýsová, Ľ. Jelemenský, M. Vrabeľ, Design, Scale-Up, and Construction of Drinking Water Recarbonization Fluidized Bed Reactor System, Processes. 10 (2022). https://doi.org/10.3390/pr10102068.

[21]	M.G. Biyoune, A. Atbir, H. Bari, L. Hassnaoui, E. Mongach, A. Khadir, L. Boukbir, R. Bellajrou, M. Elhadek, Remineralization of permeate water by calcite bed in the Daoura’s plant (south of Morocco), Eur. Phys. J. Spec. Top. 226 (2017) 931–941. https://doi.org/10.1140/epjst/e2016-60181-6.

[22]	D. Hasson, L. Fine, A. Sagiv, R. Semiat, H. Shemer, Modeling Remineralization of Desalinated Water by Micronized Calcite Dissolution, Environ. Sci. Technol. 51 (2017) 12481–12488. https://doi.org/10.1021/acs.est.7b03069.

[23]	M.G. Biyoune, B. Bouargane, H. Bari, A. Marrouche, R. Bellajrou, A. Atbir, L. Boukbir, S. Mançour Billah, Water quality depends on remineralization’s method in the desalination plant, Mediterr. J. Chem. 10 (2020) 162–170. https://doi.org/10.13171/mjc10202002141228mgb.

[24]	S. Indika, Y. Wei, D. Hu, J. Ketharani, T. Ritigala, T. Cooray, M.A.C.K. Hansima, M. Makehelwala, K.B.S.N. Jinadasa, S.K. Weragoda, R. Weerasooriya, Evaluation of performance of existing ro drinking water stations in the north central province, sri lanka, Membranes (Basel). 11 (2021). https://doi.org/10.3390/membranes11060383.

[25]	M. Mokadem, E.A. Cherif, B. Bekhti, Correction of the aggressiveness of desalinated water by mixing of treated seawater – case of Western Algeria, Int. J. Hydrol. Sci. Technol. 13 (2022) 298–304. https://doi.org/10.1504/IJHST.2022.121805.

[26]	A. Withers, Options for recarbonation, remineralisation and disinfection for desalination plants, Desalination. 179 (2005) 11–24. https://doi.org/10.1016/j.desal.2004.11.051.

[27]	A. Lesimple, F.E. Ahmed, N. Hilal, Remineralization of desalinated water: Methods and environmental impact, Desalination. 496 (2020) 114692. https://doi.org/10.1016/j.desal.2020.114692.

[28]	T. Rijnaarts, W.M. De Vos, W.G.J. van der Meer, Method for the production of drinking water, WO2020067893A1, 2020.

[29]	M. Philibert, E. Filloux, C. Garriou, D. Steinmann, A. Cipollina, Installation and process for providing mineralized drinking water, European Patent EP19306565, 2019.

[30]	M. Philibert, A. Filingeri, C. Natalello, N. Moe, E. Filloux, A. Cipollina, Surface water RO permeate remineralization through minerals recovery from brines, Desalination. 531 (2022) 115725. https://doi.org/10.1016/j.desal.2022.115725.

[31]	A. Filingeri, M. Philibert, E. Filloux, N. Moe, A. Poli, A. Tamburini, A. Cipollina, Valorization of surface-water RO brines via Assisted-Reverse Electrodialysis for minerals recovery: Performance analysis and scale-up perspectives, Desalination. 541 (2022) 116036. https://doi.org/10.1016/j.desal.2022.116036.

[32]	V. V. Wagholikar, H. Zhuang, N.E. Moe, J. Barber, H. Ramanan, J.Y.H. Fuh, Analysis of RED/dRED stack performance using a resistances in series model, Desalination. 496 (2020) 114505. https://doi.org/10.1016/j.desal.2020.114505.

[33]	L. Gurreri, M. La Cerva, J. Moreno, B. Goossens, A. Trunz, A. Tamburini, Coupling of electromembrane processes with reverse osmosis for seawater desalination: Pilot plant demonstration and testing, Desalination. 526 (2022) 115541. https://doi.org/10.1016/j.desal.2021.115541.

[34]	M. La Cerva, L. Gurreri, A. Cipollina, A. Tamburini, M. Ciofalo, G. Micale, Modelling and cost analysis of hybrid systems for seawater desalination: Electromembrane pre-treatments for Reverse Osmosis, Desalination. 467 (2019) 175–195. https://doi.org/10.1016/j.desal.2019.06.010.

[35]	Z.Y. Guo, Z.Y. Ji, Q.B. Chen, J. Liu, Y.Y. Zhao, F. Li, Z.Y. Liu, J.S. Yuan, Prefractionation of LiCl from concentrated seawater/salt lake brines by electrodialysis with monovalent selective ion exchange membranes, J. Clean. Prod. 193 (2018) 338–350. https://doi.org/10.1016/j.jclepro.2018.05.077.

[36]	H. Strathmann, Electrodialysis, a mature technology with a multitude of new applications, Desalination. 264 (2010) 268–288. https://doi.org/10.1016/j.desal.2010.04.069.

[37]	A. Campione, L. Gurreri, M. Ciofalo, G. Micale, A. Tamburini, A. Cipollina, Electrodialysis for water desalination: A critical assessment of recent developments on process fundamentals, models and applications, Desalination. 434 (2018) 121–160. https://doi.org/10.1016/j.desal.2017.12.044.

[38]	G.J. Doornbusch, M. Bel, M. Tedesco, J.W. Post, Z. Borneman, K. Nijmeijer, Effect of membrane area and membrane properties in multistage electrodialysis on seawater desalination performance, J. Memb. Sci. 611 (2020) 118303. https://doi.org/10.1016/j.memsci.2020.118303.

[39]	A. Filingeri, L. Gurreri, M. Ciofalo, A. Cipollina, A. Tamburini, G. Micale, Elucidating the current distribution along electrodialysis stacks and its influence on the current-voltage curve: behaviour from near-zero current to limiting plateau, Desalination. 556 (2023) 116541. https://doi.org/10.1016/j.desal.2023.116541.

[40]	A.M. Hulme, C.J. Davey, S. Tyrrel, M. Pidou, E.J. McAdam, Scale-up of reverse electrodialysis for energy generation from high concentration salinity gradients, J. Memb. Sci. 627 (2021) 119245. https://doi.org/10.1016/j.memsci.2021.119245.

[41]	S. Mehdizadeh, Y. Kakihana, T. Abo, Q. Yuan, M. Higa, Power Generation Performance of a Pilot-Scale Reverse Electrodialysis Using Monovalent Selective Ion-Exchange Membranes, Membranes (Basel). 11 (2021) 27. https://doi.org/10.3390/membranes11010027.

[42]	M. Vanoppen, E. Criel, G. Walpot, D.A. Vermaas, A. Verliefde, Assisted reverse electrodialysis—principles, mechanisms, and potential, Npj Clean Water. 1 (2018). https://doi.org/10.1038/s41545-018-0010-1.

[43]	S. Pal, R. Mondal, S. Guha, U. Chatterjee, S.K. Jewrajka, Crosslinked terpolymer anion exchange membranes for selective ion separation and acid recovery, J. Memb. Sci. 612 (2020) 118459. https://doi.org/10.1016/j.memsci.2020.118459.

[44]	P. Goel, E. Bhuvanesh, P. Mandal, V.K. Shahi, A. Bandyopadhyay, S. Chattopadhyay, Di-quaternized graphene oxide based multi-cationic cross-linked monovalent selective anion exchange membrane for electrodialysis, Sep. Purif. Technol. 276 (2021) 119361. https://doi.org/10.1016/j.seppur.2021.119361.

[45]	D. V. Golubenko, A.B. Yaroslavtsev, Effect of current density, concentration of ternary electrolyte and type of cations on the monovalent ion selectivity of surface-sulfonated graft anion-exchange membranes: modelling and experiment, J. Memb. Sci. 635 (2021) 119466. https://doi.org/10.1016/j.memsci.2021.119466.

[46]	J. Liao, X. Yu, N. Pan, J. Li, J. Shen, C. Gao, Amphoteric ion-exchange membranes with superior mono-/bi-valent anion separation performance for electrodialysis applications, J. Memb. Sci. 577 (2019) 153–164. https://doi.org/10.1016/j.memsci.2019.01.052.

[47]	I.A. Stenina, P.A. Yurova, L. Novak, A.R. Achoh, V.I. Zabolotsky, A.B. Yaroslavtsev, Improvement of ion conductivity and selectivity of heterogeneous membranes by sulfated zirconia modification, Colloid Polym. Sci. 299 (2021) 719–728. https://doi.org/10.1007/s00396-020-04800-7.

[48]	M. Irfan, T. Xu, L. Ge, Y. Wang, T. Xu, Zwitterion structure membrane provides high monovalent/divalent cation electrodialysis selectivity: Investigating the effect of functional groups and operating parameters, J. Memb. Sci. 588 (2019) 117211. https://doi.org/10.1016/j.memsci.2019.117211.

[49]	B. Cohen, N. Lazarovitch, J. Gilron, Upgrading groundwater for irrigation using monovalent selective electrodialysis, Desalination. 431 (2018) 126–139. https://doi.org/10.1016/j.desal.2017.10.030.

[50]	P. Zimmermann, Ö. Tekinalp, S.B.B. Solberg, Ø. Wilhelmsen, L. Deng, O.S. Burheim, Limiting current density as a selectivity factor in electrodialysis of multi-ionic mixtures, Desalination. 558 (2023). https://doi.org/10.1016/j.desal.2023.116613.

[51]	S. Ozkul, J.J. van Daal, N.J.M. Kuipers, R.J.M. Bisselink, H. Bruning, J.E. Dykstra, H.H.M. Rijnaarts, Transport mechanisms in electrodialysis: The effect on selective ion transport in multi-ionic solutions, J. Memb. Sci. 665 (2023) 121114. https://doi.org/10.1016/j.memsci.2022.121114.

[52]	Y.D. Ahdab, D. Rehman, J.H. Lienhard, Brackish water desalination for greenhouses: Improving groundwater quality for irrigation using monovalent selective electrodialysis reversal, J. Memb. Sci. 610 (2020) 118072. https://doi.org/10.1016/j.memsci.2020.118072.

[53]	Y.D. Ahdab, D. Rehman, G. Schücking, M. Barbosa, J.H. Lienhard, Treating Irrigation Water Using High-Performance Membranes for Monovalent Selective Electrodialysis, ACS Environ. Sci. Technol. Water. 1 (2021) 117–124. https://doi.org/10.1021/acsestwater.0c00012.

[54]	Y.D. Ahdab, G. Schücking, D. Rehman, J.H. Lienhard, Treatment of greenhouse wastewater for reuse or disposal using monovalent selective electrodialysis, Desalination. 507 (2021) 115037. https://doi.org/10.1016/j.desal.2021.115037.

[55]	X. Xu, Q. He, G. Ma, H. Wang, N. Nirmalakhandan, P. Xu, Selective separation of mono- and di-valent cations in electrodialysis during brackish water desalination: Bench and pilot-scale studies, Desalination. 428 (2018) 146–160. https://doi.org/10.1016/j.desal.2017.11.015.

[56]	X. Xu, L. Lin, G. Ma, H. Wang, W. Jiang, Q. He, N. Nirmalakhandan, P. Xu, Study of polyethyleneimine coating on membrane permselectivity and desalination performance during pilot-scale electrodialysis of reverse osmosis concentrate, Sep. Purif. Technol. 207 (2018) 396–405. https://doi.org/10.1016/j.seppur.2018.06.070.

[57]	X. Xu, Q. He, G. Ma, H. Wang, N. Nirmalakhandan, P. Xu, Pilot demonstration of reclaiming municipal wastewater for irrigation using electrodialysis reversal: Effect of operational parameters on water quality, Membranes (Basel). 11 (2021). https://doi.org/10.3390/membranes11050333.

[58]	E. V. Laktionov, N.D. Pismenskaya, V. V. Nikonenko, V.I. Zabolotsky, Method of electrodialysis stack testing with the feed solution concentration regulation, Desalination. 151 (2003) 101–116. https://doi.org/10.1016/S0011-9164(02)00988-8.

[59]	A. Filingeri, J. Lopez, A. Culcasi, T. Leon, A. Tamburini, J. Luis Cortina, G. Micale, A. Cipollina, In-depth insights on multi-ionic transport in Electrodialysis with bipolar membrane systems, Chem. Eng. J. 468 (2023). https://doi.org/10.1016/j.cej.2023.143673.

[60]	Y. Marcus, Ionic Radii in Aqueous Solutions, Chem. Rev. 88 (1988) 1475–1498. https://doi.org/10.1021/cr00090a003.